## Slide 1: Pixel Design and Technologies for Time-of-Flight Sensors
Tohru Yamada, Takuya Asano
Image Sensor Division
Semiconductor Business Division
Automotive & Industrial Systems Company
Panasonic Corporation
10 March 2014
Notes: Thank you, Mr. Chairman. Good afternoon, ladies and gentlemen. I am Tohru Yamada from Kyoto, Japan.
Thank you for the opportunity to present to you, today.
I work in the Image Sensor Division of the Semiconductor Business Division of Panasonic’s Automotive and Industrial Systems Company.
Sorry about the long and complicated department name.
Before we get into the presentation, let me briefly introduce my credentials.
I have some 20 years’ experience in image sensor field.
Currently, I am responsible for steering development and mass-production of image sensor products including ToF sensors.
My area of expertise is design and development of Image sensor pixels.
Today, I want to outline state-of-the-art design and technologies for enhancing pixel performance in ToF sensors.
I believe that our new technologies will help to revolutionize TOF sensor design and performance and realize prospective new applications and new markets.

## Slide 2
1. Introduction
2. Principle of Pulsed Time-of-Flight (ToF)
3. Comparison of Global Shutter Pixels
4. Pixel Design and Technologies for ToF Sensors
5. Technology for Future ToF Sensors
6. Summary
Outline
Notes: My presentation will cover five main topics.
First, I will talk about the background to this development activity. Then, I want to cover the basic principle of pulsed ToF.
Third, I'll show you comparison of global shutter pixel performances (and some benchmark results) regarding GS-CIS and IT-CCD (respectively).
Fourth, I will present design and technologies aimed at enhancing the pixel performances of ToF sensors.
Finally, I want to introduce under-development technology for future ToF sensor design and creation.
I will conclude with a summary of this presentation.

## Slide 3
Requirements for IS
Applications
Market demands
After
Before
DSC, DVC, Smartphone
High-quality 2D Visible Imaging
Accurate 3D Imaging
(Depth, Shape, Color)
Object Recognition
Classification
Picture Viewing, Recording, sharing
Consumer
Automobile
Natural U/I
Autonomous
Driving
Industry
Picture Shooting
and Recording
Visible light
Visible light and Infrared (IR) light
Entry of 3D imagers to Gaming market creates new applications
for Consumer, Industrial and Automotive markets.
3D imaging technologies will become as pervasive as 2D-DSCs
Market Trends of Image Sensors
Robotic vision
@Microsoft XBOX
@KIVA Systems
Notes: Let's start with the background to our ToF sensor development activity.
This slide shows market trends of the image sensor industry.
To date, our main market for image sensors has been DSCs, DVCs and smart phone cameras for picture shooting and recording.
These applications require high-quality 2D visible pictures and it is through pursuit of this quality that IS technologies have progressed dynamically over about a decade.
However, added value for achieving high-quality pictures has reached satisfaction level and new added value applications are being eagerly sought by the IS industry.
Entery of 3D imagers to the gaming market, in such forms as natural user interfaces, leads to creation of new applications not only in the consumer market but also in the industrial and automotive markets for development of robotic vision, autonomous driving, and so on.
In these applications, accurate 3D imaging is required for IS in order to implement object recognition and classification.
I believe that, in the near future, 3D imaging will become as pervasive a range of technologies as conventional 2D applications and the ToF sensor is a strong candidate for 3D imaging.

## Slide 4: Panasonic Image Sensors
Digital AV
Security/Automotive
Broadcast
Medical
CMOS (CIS)
Image Sensor
IT-CCD*
Small Pixel
High Sensitivity
Color Reproducibility
Small Die Size
Global Shutter
Low Smear
High IR Sensitivity
Wide Dynamic Range
Enhancing 2D imaging technologies will make further progress on ToF sensors
*Interline Transfer CCD
νMaicovicon®
SmartFSI®
Notes: Now, let me introduce Panasonic image sensors.
The Automotive and Industrial Systems Company is a unique business which has developed both CCDs and CISs.
We have more than 30 years’ experience in the IS field and have developed a number of IS products and technologies for various applications.
These applications have required us to achieve high performance levels in such areas as small pixels and high sensitivity for digital AV, high IR sensitivity and [a ]wide dynamic range for security and automotive applications, global shutter and low smear for professional broadcast cameras, and good color reproducibility and small die size for medical endoscope.
We have been able to satisfy these requirements by developing a number of standout technologies, which we believe will help us make further progress in ToF sensor development.

## Slide 5
Basic Principle of Pulsed ToF
IR Pulse
Projection
Reflection
Distance Z
Depth Calculation
High IR Sensitivity -> Long Distance Ranging
Fast Global Shutter (GS) -> Accurate Depth Measurement
Global Shutter
S0 exposure
S1 exposure
Tp
Δｔ
Projection
Light
Reflection
Light
S1
Δｔ
Tp
S0
t
t
Requirements for Pulsed ToF Pixels
Revolutionized IT-CCD pixel will satisfy these requirements
Δt
C
TP
: Time of Flight
: Light Speed
: IR Pulse width
TOF
sensor
IR
light
Notes: Now, let's take a look at the basic principle of Pulsed ToF.
In Pulsed ToF, IR pulse light is projected to the object and reflected light is captured using the global shutter of a ToF sensor.
In this operation, the ToF sensor captures two individual signals of S0 and S1 exposures.
Depth is easily calculated by dividing S1 signals by S0 signals.
The requirements for Pulsed TOF pixels are as follows:
First, reflected light intensity is inversely proportional to the square of the distance, then higher IR sensitivity is necessary for carrying out long distance ranging.
Second, a fast global shutter is very important, especially for pulsed ToF, in order to measure accurate depth.
And, our revolutionized IT-CCD pixel will satisfy these requirements.

## Slide 6
6
 | GS-CIS (5-Tr. type*) 1/3" WVGA (752x480) 6.0um□ | Panasonic IT-CCD (MN39784) 1/3" qHD (960x540) 5.4um□
Pixel Architecture |  | 
Signal Storage Region | CFD (Floating Diffusion Capacitance) | VCCD (Vertical CCD)
Overflow Control /Electronic Shutter | LOD (Lateral Overflow Drain) | VOD (Vertical Overflow Drain)
Sensitivity (@550nm) | 4.8V/lux･s (1) | 6.3V/lux･s
Parasitic Sensitivity /Smear | 0.5% / -46dB (2) | 0.0003% / -130dB
Dark Current (@25℃) | 14mV/s (1) | 0.5mV/s
Crosstalk (IR Light) | Several pixels ( p--sub.) | Within one pixel ( n--sub.)
PD
AMP
p-
CFD
↑
Many Defects
TG
PD
p-
n-
VCCD
↑
Defect-free
Photo-Shield
TG
Reference :(1)Data sheet (2)IIWS2005
Photo-Shield
LOD
OFG
VOD
Pixel performances
Global Shutter Pixels – GS-CIS vs. IT-CCD
VCCD
LOD
CFD
AMP
PD
PD
AMP
IT-CCD provides better performance in Sensitivity, Smear, Dark Current and Crosstalk.
*RST-Tr, SEL-Tr are not shown
n
n
n
Small PD Area
Large PD Area
Notes: Before getting on to current ToF pixel technologies, let me mention global shutter pixels.
This chart shows a comparison of pixel architectures and performances between the GS-CIS and our IT-CCD.
This CIS consists of 5-Tr, TG, OFG, AMP, which are indicated in this figure, and RST and SEL, which are not shown here.
CFD works as the signal storage region. Overflow control and electronic shutter are conducted by OFG.
Even though 5-Tr. GS-CIS has the smallest number of Tr. in pixels among the other GS-CIS architectures, these plural Trs. and diffusion layers make the PD area smaller, which results in decreased photo-sensitivity.
Furthermore, poor photo-shield causes serious parasitic sensitivity in the FD, defects in the FD generate large dark current, and p-type substrate, which is often used to obtain higher IR sensitivity in ToF sensors, induces a good deal of pixel crosstalk when IR light penetrates deeply into the substrate.
In contrast, IT-CCD consists of only PD and VCCD. That's all. OFD is vertically formed by using an n-substrate and a p-well which is formed by high energy I/I.
Even though this 3D pixel design is a little difficult to achieve, IT-CCD pixel is the simplest architecture for the global shutter function.
The large PD area achieves high sensitivity at visible light, and good coverage photo-shield reduces parasitic sensitivity to a negligible level.
VCCDs work as very low dark current signal storage regions. The VOD structure can suppress bulk crosstalk of IR signals to within one pixel.

## Slide 7
7
Panasonic IT-CCD (MN39784)
1/3" qHD (960x540) 5.4um□
GS-CIS 1/3" WVGA
(752x480) 6.0um□
LED light
Electric fan blade
Camera
Shutter 1/2000s
0.00003%
(-130dB)
0.5%(-46dB)
Good photo-shield of IT-CCD reduces parasitic sensitivity in VCCD; no image artifact caused by LED light can be seen.
Smear (Parasitic Sensitivity) – GS-CIS vs. IT-CCD
PD n
p-
n-
VCCD
Good Coverage
TG
n
PD
AMP
p-
CFD
TG
Poor Coverage
LOD
OFG
n
30fps
15fps
7.5fps
60fps
60fps
Notes: Now, let's take a look at some benchmark results for the GS-CIS and our IT-CCD.
The first one is smear or parasitic sensitivity.
In this comparison, an LED light is mounted on an electric fan blade and the blade is fast-rotated.
As you can see in these pictures, good photo-shield coverage in the IT-CCD can dramatically reduce parasitic sensitivity in the VCCD. No image artifacts caused by LED light can be seen in the picture.
But, with GS-CIS, poor photo-shield coverage causes significant parasitic sensitivity in the FD, which produces serious image artifacts in the direction that the LED light moves.

## Slide 8
8
16.7ms
(60fps)
33ms
(30fps)
66.7ms
(15fps)
IT-CCD (MN39784)
GS-CIS
Readout time
Sensor temperature 80 degrees; exposure time 1/10000s
Dark Current – GS-CIS vs. IT-CCD
n
n++
CFD
PD
TG
AMP
Junction Defect
Bulk Defect
p++
n
n
VCCD
PD
p-
Defect-free
p++
IT-CCD
GS-CIS
TG
VCCD of IT-CCD has low doped channel and no metal junction; this can reduce surface and bulk defects, resulting in low dark current.
n-
p-
Notes: Next, we have a dark current comparison.
Here the sensor temperature is set to 80 degrees. Three different readout time images are shown in this slide.
GS-CIS stores the signals in the FD, which has a number of junction defects due to the metal contact and a number of bulk defects due to high doped ion-implantation, which causes serious white blemishes and dark current.
While IT-CCD stores the signals in the VCCD, which has a low doped channel and no metal junction, this can reduce generation of surface and bulk defects, resulting in suppression of white blemishes and dark current.

## Slide 9
9
960 pixels
540 pixels
Resolution chart of IT-CCD taken by IR light has Good Resolution.
VOD structure can suppress Bulk Crosstalk by Drift transfer of Photo-electrons.
Good Resolution
IR light = 850nm
IR Image Resolution – GS-CIS vs. IT-CCD
Blurred Image
752 pixels
540 pixels
IT-CCD (MN39784)
5.4um□
GS-CIS
6.0um□
200 pixels
200 pixels
SUB (p-)
PD
IR Light
n
SUB (n-)
PD
p
IR Light
n
VOD Barrier
Diffusion
Drift
Drift
Notes: Finally, here is a comparison of IR Image resolution.
Here, the wavelength of the IR light is 850nm. IR images of resolution charts are captured for both sensors.
As you can see in these enlarged pictures, a blurred image is obtained for GS-CIS. This is due to the bulk crosstalk caused by thermal diffusion of the photo-electrons generated in the deep part of the p-type substrate.
While IT-CCD pixels have VOD structure, photo-electrons generated above VOD barriers are immediately transferred to each target PD by electrical field drift, and electrons generated below the VOD barriers drain to the n-substrate. This can suppress bulk crosstalk and enable reproduction of the original resolution.

## Slide 10
10
Pixel Design and Technologies for ToF Sensors
Advantages of IT-CCD pixels
  High Sensitivity (@Visible Light)
  Low Parasitic Sensitivity (Low Smear)
  Low Dark Current
  Low Crosstalk (@IR Light)
Approach
  High Reflective-Index Micro-Lens
  Deep PD w/ VOD
  Electric Field Enhancement in the Deep PD
Metal
TG
Metal
TG
Challenges for ToF Sensor
  1. Long Distance Ranging
    High Fill-Factor (Effective FF=70%@5.4um□)
    Enhanced IR Sensitivity (Q.E.=18%@850nm)
  2. Accurate Depth Measurement
    Electronic Fast Shutter (tr, tf<2nsec)
Electric Field
Enhancement
Deep
PD
VCCD
Deep
VOD
Barrier
Deep Narrow
Isolation
(NI)
High Reflective-Index (HRI)
Micro-Lens
Notes: Now, I want to talk about state-of-the-art pixel design and technologies for ToF sensors.
As explained in the previous slides, the IT-CCD pixel has the advantages of high sensitivity at visible light, low parasitic sensitivity, low dark current and low crosstalk in the IR.
Despite these advantages, we need to revolutionize our IT-CCD pixels in order to address the following challenges to further progress on ToF sensors.
First, in order to achieve long distance ranging, the High Reflective-Index micro-lens and Deep PD have been developed. The resulting effective FF is 70% and the QE in the IR is 18%.
Second, Electric Field Enhancement in the Deep PD is implemented in order to realize an electronic fast shutter for accurate depth measurement. The resulting rise time and fall time of the shutter pulse are shorter than 2nsec.
Today I will introduce the last two approaches.

## Slide 11
Enhanced IR Sensitivity – Deep PD w/ VOD
IR Light penetrates deeply into Si substrate.
Deep PD is necessary to obtain
higher IR sensitivity.
Deep PD is created by forming Deep VOD Barrier and Deep Narrow Isolation through High-Energy Ion-Implantation process.
Light absorptivity [a.u.]
Depth of Si [um]
Light Absorptivity in Si
Conventional PD
PD (n)
SUB (n-)
2
Deep PD
Deep
PD
SUB (n-)
Deep VOD Barrier (p)
VCCD
VOD Barrier (p)
Potential
(p)
Potential
Deep Narrow Isolation
VCCD
Quantum Efficiency (Q.E.)
Wavelength [nm]
x 2.8
Q.E. [a.u.]
Conventional PD
Deep PD
18%
(n)
Conventional PD
Deep PD
λ=850nm (IR)
450nm
550nm
650nm
Pixel Impurity Profiles
Notes: Let me show you the new technology for enhancing IR sensitivity.
This graph shows the light absorptivity in Si. As you can see, IR light absorptivity is very low, so IR light penetrates deeply into the Si substrate.
Then, Deep PD is necessary to obtain higher IR sensitivity. The Deep PD is created by forming a deep VOD barrier and deep narrow isolation through a high-energy ion-implantation process.
The VOD barrier of the Deep PD is deepened from 3um to 5um and the resulting Q.E.@850nm is increased to 18%, or 2.8-times higher than that of the conventional PD.

## Slide 12
12
Deep PD w/ VOD
P-sub. structure
Even though p-sub. obtains higher DC at ST longer than 16nsec, the DC plummets as ST becomes shorter, while Deep PD w/ VOD retains DC and 90% of it is obtained at ST of 500psec.
PD
(n)
SUB(n-)
VOD Barrier (p)
VCCD
1
2
VCCD
PD
(n)
SUB(p-)
1
2
TG pulse
IR pulse
(850nm)
OFF
ON
OFF
ON
Shutter Time (ST) :0.5nsec ~ 1000nsec
Photo-current [a.u.]
Photo-current [a.u.]
Time [nsec]
Time [nsec]
IR pulse
TG pulse
TG pulse
IR pulse
1. Photo-electrons are generated in PDs and transferred to VCCDs.
2. After TG pulse turns off, electrons in deep regions of substrate belatedly move to PD.
PD signals
VCCD
signals
Shutter Time (ST) [nsec]
Demodulation Contrast (DC)
( VCCD sig. - PD sig. ) [a.u.]
Shutter ON (1)
OFF (2)
500psec
@90%
Potential
Potential
Drift
Diffusion
Deep PD w/ VOD
P-sub.
16nsec
Fast Shutter Simulations
VCCD
signals
PD signals
ON (1)
OFF (2)
Photo-Current Simulations
10nsec
Fast Shutter Characteristics– Deep PD w/ VOD
Notes: Next, I want to discuss the fast shutter simulation results of the deep PD with VOD compared to the p-sub. structure.
These analyses are conducted using transient photo-current simulations.
In order to simplify analysis, both structures have the same VCCDs and PDs. Only the substrate type and VOD barrier of the Deep PD structure are different from those of the p-sub. structure.
For both structures, TG pulses are applied to the transfer gates from 0.5nsec to 1000nsec and 850nm IR pulses are synchronized with TG pulses .
As you can see in the photo-current simulation results for Deep PD with VOD, during the shutter-on period, photo-electrons are generated in the PD and almost all of these electrons are instantly transferred to the VCCDs through electric field drift. Then, after the TG pulse turns off, PD signals remain at negligible levels.
But, in the case of the p-sub. structure, during the shutter-on period, photo-electrons are generated and gradually transferred to the VCCDs through thermal diffusion. Even after the TG pulse turns off, electrons in deep regions of the substrate belatedly move to the PD and a significant amount of PD signals remains.
Residual PD signals degrade demodulation contrast, which is calculated by subtracting PD signals from VCCD signals.
This figure shows the simulated shutter time dependence of demodulation contrast.
The red line shows the p-sub structure and the blue line shows the Deep PD with VOD.
As you can see in this graph, even though the p-sub. structure obtains higher demodulation contrast at a shutter time longer than 16nsec, the demodulation contrast plummets as shutter time becomes shorter, while the Deep PD with VOD retains demodulation contrast and 90% of it is obtained at the shutter time of 500psec.

## Slide 13
13
n-
p-
n
Fast Shutter Evaluation
Photo-Response of SUB Shutter
Shutter ON
OFF
VTG=High
VSUB
Low
High
Sweep
OFF
High
Low
Potential
CR(S/N)
=80
VTG=High
S
N
Pixel Cross Section
Potential Profiles
w/ Variation
n
VOD
PD
SUB
VCCD
Pico-pulse laser
Constant IR light
CR(S/N)
=150
S
N
w/o Variation
w/ Slant
High
Low
Small VOD
Barrier shift
w/o Slant
Conventional Design
Optimum Design for TOF
VSUB
44nsec
Enhancing Electric Field Modulation and Suppressing VOD Barrier Shift through a VSUB change can remove the Variation and the Slant of Photo-Response and improve the CR at the same time.
Photo-Response [a.u.]
Large VOD
Barrier shift
Time [nsec]
Time [nsec]
VTG=High
VSUB
VSUB
tr=
1.8ns
tf=
1.1ns
Potential
Pixel Design for Fast Shutter in Deep PD w/ VOD
Shutter
OFF
ON
Shutter
OFF
ON
Notes: Now, let me explain pixel design for achieving fast shutter in the deep PD with VOD.
These figures show the pixel cross-section and fast shutter evaluation method.
In this evaluation, the TG voltage is set to a high level and constant IR light is applied.
High SUB voltage is applied to the substrate during the shutter-off period; low SUB voltage is applied during the shutter-on period.
A Pico-pulse laser is activated and swept during shutter-off and shutter-on periods. This can obtain PD photo-responses of the sub shutter.
The photo-response of the SUB shutter and potential profiles along the dash line are shown for both conventional pixel design and optimal pixel design for ToF.
As you can see in the above photo-response graph, there are three challenges for conventional design.
The first of these is the slant at the rise edge, which is caused by variation in PD sensitivity due to the large shift of the VOD barrier as the transition of SUB voltage.
The second challenge is the pixel-to-pixel variation at the fall edge, which is caused by transfer inefficiency due to lack of a fringing field from the VOD barrier to the VCCD in the last second of the shutter-on period.
The final one is the low contrast ratio, which is calculated by dividing Signal by Noise. The noise is generated during the shutter-off period by the leakage of photo-electrons from the PD due to the low fringing field from the PD to the SUB.
To overcome these challenges, we have implemented optimal pixel design for TOF.
Enhancing Electric Field modulation in the Deep PD and suppressing VOD barrier shift through a SUB voltage can successfully remove the variations and slants in photo-response and improve the CR at the same time.

## Slide 14
Shutter Time (ST) [nsec]
Demodulation Contrast (DC)
Deep PD w/VOD
P-sub.
Double Deep PD w/VOD
Double Deep PD realizes 1.6 times higher IR sensitivity than Deep PD. DC of this PD will surpass P-sub. at ST <500nsec. Slants and Variations could be removed through optimum pixel design.
Fast Shutter Simulations
500nsec
Technology for Future TOF – Double Deep PD
Quantum Efficiency (Q.E.)
CR(S/N)
=150
S
N
w/o Variation
w/o Slant
CR(S/N)
=130
x1.6S
N
w/ Variation
w/ Slant
Photo-Response [a.u.]
Time [nsec]
Time [nsec]
Q.E. [a.u.]
Wave Length [nm]
x 1.6
Deep PD
Double Deep PD
28%
Deep PD
PD (n)
SUB(n-)
Deep VOD Barrier
VCCD
(p)
Deep Narrow Isolation
Double Deep PD
PD (n)
SUB(n-)
Double Deep
VOD Barrier
VCCD
(p)
Double Deep NI
Photo-Response of SUB Shutter
Optimized Deep PD
Double Deep PD
(p)
(p)
Notes: Let's move on to the approach for future ToF sensors.
We currently have under development Double Deep PD, using ultra high energy ion implantation and epitaxial growth technologies.
The first trial production of Double Deep PD obtains 1.6-times higher IR sensitivity than that for the Deep PD I shown in the previous slide.
Fast shutter simulations indicate that the demodulation contrast of the double deep PD will surpass that of the p-sub. structure at a shutter time shorter than 500nsec. This will be a major advantage of the Double Deep PD for longer distance ranging and accurate depth measurement through the generally used ToF shutter time.
Unfortunately slant and pixel to pixel variation of photo-response remain in the first trial production. These could be removed through optimal pixel design.

## Slide 15
15
Summary
This work
  1-1. High Reflective-Index Micro-Lens -> High F.F. (70%@5.4um□)
  1-2. Deep PD w/ VOD -> High IR Q.E. (18%@850nm)
  2. Electric Field Enhancement in the Deep PD -> Fast Shutter (tr, tf<2nsec)
Requirements for Pulsed ToF
  1. High IR Sensitivity -> Long Distance Ranging
  2. Fast Global Shutter -> Accurate Depth Measurement
Advantages of IT-CCD Pixel
  Better performance in areas of Sensitivity, Smear, Dark Current and Crosstalk.
Revolutionized IT-CCD pixel will aid further progress on ToF sensors
Next Approach to Future ToF
  Double Deep PD w/ VOD -> Higher IR Q.E. (28%@850nm)
IT-CCD pixel can satisfy
these requirements.
Notes: Finally let me summarize this presentation.
As I mentioned, the IT-CCD pixel has strong advantages in terms of Sensitivity, Smear, Dark Current and Crosstalk.
Pulsed ToF requires high IR sensitivity for long distance ranging and a fast global shutter for accurate depth measurement.
Our IT-CCD pixel can satisfy these requirements.
In this work, the High Reflective Index micro-lens realizes effective Fill Factor of up to 70%@5.4um□pixels.
Deep PD increases quantum efficiency to 18%@850nm.
Electric Field enhancement in the Deep PD achieves an electronic fast shutter with rise time and fall time shorter than 2nsec.
For future ToF sensors, Double Deep PD with VOD can further enhance quantum efficiency in the IR up to 28%.
Our simulation indicates that this PD will obtain higher demodulation contrast than that for the p-sub. structure through the generally used ToF shutter time.
In conclusion, we believe that our revolutionized IT-CCD pixel will aid further progress on ToF sensors and has the potential to make it the front-runner in 3D imagers.
Thank you.

## Slide 16
Thank you